Distribution Agreement

In presenting this thesis or dissertation as a partial fulfillment of the requirements for an advanced degree from Emory University, I hereby grant to Emory University and its agents the non-exclusive license to archive, make accessible, and display my thesis or dissertation in whole or in part in all forms of media, now or hereafter known, including display on the world wide web. I understand that I may select some access restrictions as part of the online submission of this thesis or dissertation. I retain all ownership rights to the copyright of the thesis or dissertation. I also retain the right to use in future works (such as articles or books) all or part of this thesis or dissertation

Signature:

_____________________________________		 __________

Jier Huang						                  Date

Charge Separation Dynamics between Semiconductor Nanoparticles and Molecular Adsorbates

By

Jier Huang

Doctor of Philosophy

Chemistry

_____________________________________

Dr. Tianquan Lian, Advisor

_____________________________________

Dr. Michael C. Heaven, Committee Member

_____________________________________

Dr. Joel M. Bowman, Committee Member

Accepted:

__________________________________

Dean of the Graduate School

Lisa A. Tedesco. Ph.D.

__________________________________

Date

Charge Separation Dynamics between Semiconductor Nanoparticles and Molecular Adsorbates

By

Jier Huang

B.S. Lanzhou University, P.R. China, 2001

M.S. Lanzhou University, P.R. China, 2004

Advisor: Tianquan Lian, Ph.D.

An abstract of

A dissertation submitted to the Faculty of the

James T. Laney School of Graduate Studies of Emory University

in partial fulfillment of the requirements for the degree of

Doctor of Philosophy

in Chemistry

2010

Abstract

Charge Separation Dynamics between Semiconductor Nanoparticles and Molecular Adsorbates

By Jier Huang

The understanding of the interfacial charge transfer dynamics between semiconductor nanoparticles and molecular adsorbates is essential to their potential applications in solar cells. In this dissertation, we investigated two types of semiconductor nanoparticle – molecular adsorbate systems: (1) quantum dots (QD)-adsorbate complexes and (2) dye sensitized semiconductor films, by using transient absorption spectroscopy and time resolved fluorescence spectroscopy.

For the first system, we conducted a series of studies on exciton dissociation dynamics in QDs through charge transfer to the adsorbed molecules. We investigated single exciton dissociation dynamics in CdSe QDs through electron transfer (ET) to a Re-bipyridyl complex, methylene blue (MB+) molecules, and Flavin mononucleotide by monitoring the spectral features of both the QDs and molecular adsorbates. It was found that the ET rate depends on the number of adsorbatess per QD as well as the QD particle size. The fastest observed ET rates were on the sub-ps time scale, which is much faster than the exciton-exciton annihilation process, indicating the possibility to dissociate multiple excitons through ET from QDs to molecular adsorbates. Additionally, we have investigated exciton dissociation dynamics in CdSe QDs through hole transfer to phenothiazine molecules (PTZ). It was shown that the hole transfer time was ～ 2.5 ns in 1:1 CdSe-PTZ complexes and reached ～ 300 ps in samples with an average of ～ 6 PTZ per QD. Furthermore, we demonstrated the capability to dissociate multiple excitons in CdSe-MB+ complex. It was shown that ～ 3 excitons in CdSe QDs can be dissociated through ET to MB+.

For the second system, we examined the ET dynamics from Rhodamine (Rh) dyes to different semiconductor films. Electron injection kinetics from RhB to In2O3, SnO2, and ZnO films were compared to examine the effect of the semiconductor nature on the ET dynamics. It was found that ET rate follows the order of In2O3 ≈ SnO2 > ZnO. Additionally, we also explored the impact of dye energetics on ET dynamics by comparing the injection kinetics from RhB, Rh101, and Rh6G to the same semiconductor. The results showed that the ET rate decreases with a decrease in the excited state oxidation potential.

.  Charge Separation Dynamics between Semiconductor Nanoparticles and Molecular Adsorbates

By

Jier Huang

B.S. Lanzhou University, P.R. China, 2001

M.S. Lanzhou University, P.R. China, 2004

Advisor: Tianquan Lian, Ph.D.

A dissertation submitted to the Faculty of the

James T. Laney School of Graduate Studies of Emory University

in partial fulfillment of the requirements for the degree of

Doctor of Philosophy

in Chemistry

2010

ACKNOWLEDGEMENT

First, I would like to express my sincere gratitude to my advisor, Professor Tianquan Lian, for his inspirational guidance and general support throughout my graduate career. His wide knowledge and logical way of thinking have been of great value to me. Without his supervision, I would not have achieved the necessary skills in experimental design and scientific reasoning, and would not have established the confidence to be a scientist. I also wish to extend sincere thanks to my graduate committee members, Dr. Michael C. Heaven and Dr. Joel M. Bowman, for their insightful comments, hard questions and valuable time.

I would like to show my gratitude to my lab fellows for their support and friendship. Dr. Jianchang Guo and Dr. Chunxing She provided guidance in my earlier graduate career. Dr. David Stockwell, from whom I learned laser skills, offered the most valuable support and friendship. Shengye Jin provided the fluorescence measurements in this thesis. Zhuangqun Huang has provided me with quantum dots for this thesis with consistent quality. Chantelle Anfuso has made herself available to offer help and suggestions whenever I need her. Ye Yang offered special help in experiments and by challenging my ideas. I am also grateful for the help from my other group members, Haimin Zhu, Nianhui Song, Dr. Abey Issac, Dr. Baohua Wu, Zhe Zhang, and David Wu.

Last but not least, I would like to thank my entire family. My parents and in-laws have given me encouragement and support when I had difficult times and gave special help in taking care of my two sons. My husband, Zhihui Zhang, has given me unlimited love and support by encouraging me at every step of the way. My two lovely sons, Ethan and Andrew, have provided me with happiness and understanding.

Table of Contents

| Chapter 1. Introduction......................................................................................... |  | 1 |
| --- | --- | --- |
|  | - Ultrafast Exciton Dissociation in CdSe Quantum Dots through Charge Transfer to Molecular Adsorbates................................................................ - Introduction………………………………………………………... - Single Exciton Dissociation……………………………………….. - Multiexciton Dissociation…………………………………………. | 1 1 1 4 9 |
|  | - ET Dynamics from Molecular Adsorbates to Semiconductor Nanocrystalline Thin Films.......................................................................... | 12 |
|  | 1.3 Summary....................................................................................................... | 13 |
|  | References........................................................................................................... | 13 |

| Chapter 2. Experimental Section......................................................................... |  | 23 |
| --- | --- | --- |
|  | 2.1 Preparation of QDs and Semiconductor Thin Films.…............................... | 23 |
|  | 2.2 Preparation of QD-adsorbate Complex and Dye Sensitized Semiconductor Thin Films...................................................................................................... | 26 |
|  | 2.3 Spectroscopic Measurement…………………………….………………… | 28 |
|  | References........................................................................................................... | 30 |

| Chapter 3. Exciton Dissociation Dynamics in CdSe Quantum Dots by Electron Transfer to Re-bipyridyl Complexes.................................................. |  | 32 |
| --- | --- | --- |
|  | 3.1. Introduction……………………………………………………………….. | 32 |
|  | 3.2 Results………………………………………………….……………….…. | 34 |
|  | 3.2.1. Exciton Dissociation Pathway in CdSe-ReC0A Assemblies.…….... | 34 |
|  | 3.2.1.1. Static Absorption Measurement……..…………………..…… | 34 |
|  | 3.2.1.2. Fluorescence Lifetime Measurement..……….………….....… | 35 |
|  | 3.2.1.3. Transient IR Absorption Measurement………………………. | 36 |
|  | 3.2.1.4. Transient Visible Absorption Measurement………...….….… | 40 |
|  | 3.2.2. The Effect of the Number of ReC0A per QDs on ET rate.…………. | 42 |
|  | 3.2.3. The Effect of QD Particle Sizes on ET rate………………………… | 45 |
|  | 3.3 Discussion……………................................................................................. | 46 |
|  | 3.4 Summary……............................................................................................... | 48 |
|  | References……………………………………………………………………... | 49 |

| Chapter 4. Exciton Dissociation Dynamics in CdSe Quantum Dots by Electron Transfer to Flavin................................................................. |  | 51 |
| --- | --- | --- |
|  | 4.1 Introduction……………………………………………............................... | 51 |
|  | 4.2 Results………………...………………………............................................ | 53 |
|  | 4.2.1 Static Absorption Measurement……………….................................. | 53 |
|  | 4.2.2 Transient Visible Absorption Measurement..………………………. | 54 |
|  | 4.3 Summary…………………………………………………........................... | 57 |
|  | References........................................................................................................... | 57 |

| Chapter 5. Exciton Dissociation in CdSe Quantum Dots by Hole Transfer to Phenothiazine……………………………………………………….. |  | 62 |
| --- | --- | --- |
|  | 5.1 Introduction……………………………………………............................... | 62 |
|  | 5.2 Results………………...………………………............................................ | 65 |
|  | 5.2.1 Static Absorption Measurement…………………………………….. | 65 |
|  | 5.2.2 Fluorescence Lifetime Measurement……………………………….. | 66 |
|  | 5.2.3 Transient Absorption Measurement ...…………………..……..…… | 67 |
|  | 5.3 Discussion…………………………………………………………………. | 72 |
|  | 5.4 Summary....………………………………………………........................... | 76 |
|  | References........................................................................................................... | 77 |

| Chapter 6. Multiple Exciton Dissociation in CdSe through Electron Transfer to Methylene Blue……………............................................................... |  | 81 |
| --- | --- | --- |
|  | 6.1 Introduction………………………………………………………………... | 81 |
|  | 6.2 Results and Discussion .…………………………………………………... | 84 |
|  | 6.2.1 Single Exciton Dissociation Dynamics in CdSe(510nm)-MB+ Complex ……...................................................................................... | 84 |
|  | 6.2.1.1 ET Pathway in CdSe(510nm)-MB+ Complex………………... | 84 |
|  | 6.2.1.2 Energy Transfer Efficiency in CdSe(510nm)-MB+ Complex... | 89 |
|  | 6.2.2 Single Exciton Dissociation Dynamics in CdSe(510nm)-MB+ Complex ……...................................................................................... | 91 |
|  | 6.2.2.1 ET Pathway in CdSe(553nm)-MB+ Complex……………….... | 91 |
|  | 6.2.2.2 Energy Transfer Efficiency in CdSe(553nm)-MB+ Complex.... | 94 |
|  | 6.2.3 Exciton-Exciton Annihilation……..................................................... | 96 |
|  | 6.2.2.1 Quantirying Exciton-Exciton Annihilation Rate…................... | 96 |
|  | 6.2.2.2 Quantifying the Number of Excitons per QD............................ | 101 |
|  | 6.2.4 Multiexciton Dissociation…………………………………………... | 103 |
|  | 6.2.4.1 Multiexciton Dissociation Dynamics…………………………. | 104 |
|  | 6.2.4.2 Quantifying the Number of Reduced MB+ …………………... | 109 |
|  | 6.3 Summary..…………………...…………….................................................. | 111 |
|  | References........................................................................................................... | 112 |

| Chapter 7. Interfacial Electron Transfer Dynamics from Organic Dyes to Semiconductor Nanocrystalline Thin Films………………………… |  | 117 |
| --- | --- | --- |
|  | 7.1 Introduction……………………………………………………………….. | 117 |
|  | 7.2 Results…………………………………………………………………….. | 120 |
|  | 7.2.1 Effects of Semiconductors on the Injection Rate …...……………… | 120 |
|  | 7.2.1.1 Non-ET Dynamics in RhB Sensitized ZrO2 Films...…………. | 120 |
|  | 7.2.1.2 ET Dynamics in RhB Sensitized In2O3 Films………………... | 123 |
|  | 7.2.1.3 ET Dynamics in RhB Sensitized SnO2 Films………………… | 130 |
|  | 7.2.1.4 ET Dynamics in RhB Sensitized ZnO Films…………………. | 135 |
|  | 7.2.1.5 Comparison of ET from RhB to In2O3, SnO2 and ZnO Films | 141 |
|  | 7.2.2 Effects of Dye Energetics on the Injection Rate …………………… | 143 |
|  | 7.3 Discussion…………………...…………….................................................. | 145 |
|  | 7.3.1 Effects of Semiconductors on the Injection Rate…………...…….… | 145 |
|  | 7.3.2 Effects of Dye Energetics on the Injection Rate……………...…….. | 146 |
|  | 7.4 Summary…………………………………………………...……………… | 147 |
|  | References........................................................................................................... | 148 |

List of Figures

Chapter 1

| Figure 1.1 | Schematic diagram showing the configurations of (a) quantum dot solar cell with QDs dispersed in a blend of electron- and hole- conducting polymers and (b) dye sensitized solar cell. | 3 |
| --- | --- | --- |
| Figure 1.2 | Schematic diagram of exciton dissociation process in QD-adsorbate complex | 5 |
| Chapter 2 |  |  |
| Figure 2.1 | Molecular Structures of (a) ReC0A, (b) Methylene Blue, (c) Phenothiazine, (d) Rhodamine B, (e) Rhodamine 101, (f) Rhodamine 6G, and Flavin mononucleotide. | 27 |

Chapter 3

| Figure 3.1 | (a) UV-vis absorption spectra of CdSe QDs with indicated first exciton peak positions. b) FTIR spectra of ReC0A absorbed on CdSe QDs with indicated first exciton peak positions. | 34 |
| --- | --- | --- |
| Figure 3.2 | Fluorescence decay of CdSe (505nm) with indicated average number (R) of adsorbed ReC0A per QD. | 35 |
| Figure 3.3 | (a) Transient IR spectra of CdSe (435nm) -ReC0A complex in the CO stretching mode region at indicated delay times after 400 nm excitation. | 36 |
| Figure 3.4 | Comparison of electron decay kinetics of intraband transition probed in 2070cm-1 in CdSe (filled circles) and CdSe-ReC0A (open triangles) after 500 nm excitation. The inset shows the data extended to the longer time scale. Both kinetics have been normalized at the maximum amplitudes for better comparison. | 37 |
| Figure 3.5 | Comparison of electron decay kinetics of intraband transition in CdSe probed under different wavelengths after 500 nm excitation. | 39 |
| Figure 3.6 | Transient visible spectra of CdSe (a), and CdSe (505nm)-ReC0A complex (b), at indicated delay times after 400 nm excitation. | 40 |
| Figure 3.7 | Comparison of intraband transition decay kinetics (filled circles) and exciton bleach recovery kinetics (open triangles) for CdSe-ReC0A complex. The exciton bleach signal has been inverted and scaled for better comparison. The insets show the data extended to the longer time scale. | 41 |
| Figure 3.8 | FTIR spectra of ReC0A absorbed on CdSe QDs with indicated numbers of ReC0A per particle. | 42 |
| Figure 3.9 | (a) Comparison of exciton bleach recovery of CdSe-ReC0A samples after 400 nm excitation. (b) Comparison of decay kinetics of intraband transition of CdSe-ReC0A samples after 400 nm excitation. The insets show the same data extending to longer time scales. | 43 |
| Figure 3.10 | Comparison of exciton bleach recovery of CdSe-ReC0A samples for three QD sizes after 400 nm excitation. All kinetic traces have been normalized at the maximum amplitudes for better comparison. | 45 |

Chapter 4

| Figure 4.1 | UV-visible absorption spectra of CdS (389 nm) in heptane, CdSe (389 nm)-FMN complexes in heptane, and FMN in ethanol. | 54 |
| --- | --- | --- |
| Figure 4.2 | (a) Transient spectra of CdS(389nm) at indicated delay times after 400 nm excitation. (b) Transient spectra of CdSe(389nm)-FMN at indicated delay times after 400 nm excitation. The static absorption spectrum of FMN in ethanol is also shown in panel b as gray solid line. | 55 |

Chapter 5

| Figure 5.1 | (a) UV-visible absorption spectra of CdSe (sample 0) and CdSe-PTZ (samples 1-4) in heptane solution with different concentrations of PTZ. b) Difference spectra between free CdSe (sample 0) and CdSe-PTZ (samples 1-4). The absorption spectrum of PTZ in heptane (dotted line) was also shown. | 77 |
| --- | --- | --- |
| Figure 5.2 | QD fluorescence decay (dots) of sample 0 (free QDs) and samples 1-4 (CdSe-PTZ solutions) and their fits (dashed lines) according to the model described in the main text. | 78 |
| Figure 5.3 | UV-visible spectra of CdSe, CdSe-PTZ assemblies and PTZ solution in heptane. | 79 |
| Figure 5.4 | (a) Transient spectra of CdSe-PTZ assemblies (main panel) and CdSe (inset) at indicated delay times after 400 nm excitation. (b) Expanded view of the same transient spectra shown in (a). | 81 |
| Figure 5.5 | Comparison of exciton bleach recovery kinetics at 462 nm for CdSe (filled circles) and CdSe-PTZ assemblies (empty triangles). | 82 |
| Figure 5.6 | Comparison of the formation kinetics of cation absorption at 525 nm (filled circles), broad absorption decay at 570-650 nm (open squares), and fluorescence lifetime decay kinetics (black solid line) for CdSe-PTZ assemblies. The broad absorption signals and fluorescence signals have been normalized to the same initial amplitude as the cation formation signals, and have been inverted for better comparison. | 83 |

Chapter 6

| Figure 6.1 | UV-visible absorption spectra of CdSe (510 nm) and CdSe (510 nm)-MB+ complexes in heptane, and fluorescence spectra of CdSe (510 nm) QDs in heptane. | 84 |
| --- | --- | --- |
| Figure 6.2 | (a) Transient spectra of CdSe(510nm) at indicated delay times after 400 nm excitation. (b) Transient spectra of CdSe(510nm)-MB+ at indicated delay times after 400 nm excitation. (c) Comparison of exciton bleach recovery kinetics of CdSe-MB+ assemblies at 505-515 nm (black triangles) and the depletion kinetics of MB+ in the ground state (red circles). | 85 |
| Figure 6.3 | (a) Transient spectra of CdSe(470nm) at indicated delay times after 400 nm excitation. (b) Transient spectra of CdSe(470nm)-MB at indicated delay times after 400 nm excitation. (c) Comparison of exciton bleach recovery kinetics of MB-CdSe assemblies at 465-475 nm (black triangles) and the depletion kinetics of MB in the ground state (red circles). | 88 |
| Figure 6.4 | Emission spectra of CdSe (510nm) and CdSe(510nm)-MB+ complexes The insets show the expanded view of these spectra as well as MB+ emission spectra obtained according to the approach described in the main text. | 89 |
| Figure 6.5 | UV-visible absorption spectra of CdSe (553 nm) and CdSe (553 nm)-MB+ complex. | 91 |
| Figure 6.6 | (a) Transient visible spectra of CdSe (553 nm) at indicated delay times after 400 nm excitation. (b) Transient visible spectra of CdSe(553 nm)-MB+ complexes at indicated delay times after 400 nm excitation. The spectra were measured with excitation pulse energy of 11 nJ. | 92 |
| Figure 6.7 | Comparison of the recovery kinetics of QD 1S exciton bleach (black open triangles) and the formation kinetics of MB+ ground state bleach (red open circles) in CdSe-MB+ complexes. Also shown is the exciton bleach recovery kinetics of QD only (blue filled circles). The MB+ ground state bleach signal has been normalized and inverted for better comparison. | 93 |
| Figure 6.8 | a) UV-vis absorption spectra of CdSe in heptane (solid black line), CdSe-MB+ in heptane (red dashed line) and MB+ in ethanol (blue dash-dot line). b) Static emission spectra of CdSe in heptane (solid black line), CdSe-MB+ in heptane (red dashed line) and MB in ethanol (blue dash-dot line) after 450 nm excitation. | 94 |
| Figure 6.9 | Comparison of transient visible absorption spectra of CdSe (553nm) complexes at indicated delay times after 400 nm excitation for various excitation energy (as indicated). | 97 |
| Figure 6.10 | Comparison of (a) 1S and b) 1P exciton bleach recovery kinetics of CdSe(553 nm) at indicated excitation energy. Kinetic traces have been normalized to the same value at 1ns. The left panel shows the data up to 10 ps in linear scale and the right panel displays the data from 10 ps to 1ns in logarithmic scale. | 98 |
| Figure 6.11 | (a) Excitation power dependence of the exciton bleach amplitude at t = 1 ps (red open circles) and t = 1 ns (black solid circles) in QDs. (b) Excitation power dependence of the normalized exciton bleach amplitude at t = 1 ps (red open circles) and t = 1 ns (black solid circles) in QDs. | 102 |
| Figure 6.12 | Comparison of transient visible absorption spectra of CdSe-MB+ complexes at indicated delay times after 400 nm excitation for various excitation energy (as indicated). | 104 |
| Figure 6.13 | Comparison of the kinetics of (a) MB+ bleach formation, b) 1S exciton bleach recovery and c) 1P exciton bleach recovery in CdSe-MB+ at indicated excitation energy. Also shown in b) and c) are the 1S and 1P exciton bleach recovery in CdSe only at the highest excitation energy (blue dashed line). All kinetic traces have been normalized to the same maximum amplitude. The left panel shows the data up to 10 ps in linear scale and the right panel displays the data from 10 ps to 1ns in logarithmic scale. | 105 |
| Figure 6.14 | Excitation power dependence of the amplitudes of normalized MB+ bleach in QD-MB+. The normalized exciton bleach at t = 1ps (red open circles) and t = 1ns (black solid circles) in QDs as a function of excitation power are also shown here. Solid line is the average number of excitons per QD and dashed lines are fits according to equation 6.5. The curves for nmax=1 and 2 (equation 4) are the same as those for S1S(T) and S1S(0) (equation 6.4), respectively. Normalized QD bleach signals are defined in equation (2) and the MB+ bleach signal is normalized such that it equals to the normalized QD 1S exciton bleach signal at the lowest excitation energy. | 109 |

Chapter 7

| Figure 7.1 | Transient visible absorption spectra of RhB/ZrO2 at indicated delay times after excitation at 532 nm. Also plotted along the negative vertical axis is the ground state absorption (GSA) of RhB/ZrO2 (thick solid line) recorded by a static UV-vis absorption spectrometer. | 121 |
| --- | --- | --- |
| Figure 7.2 | UV-visible spectra of RhB/In2O3 films at three different coverage levels, 1 (0.1 OD), 2 (0.18 OD), and 3 (0.3 OD). All spectra were normalized to the same peak height for better comparison of peak shift. The original spectra are shown in the inset. | 123 |
| Figure 7.3 | IR transient absorption kinetic traces of RhB/In2O3 films 1-3 after 532 nm excitation. The inset shows the data extended to longer time scale. The signal sizes, which have been scaled by the number of absorbed excitation photons, reflect relative injection yields. | 124 |
| Figure 7.4 | Transient IR kinetic traces of RhB/In2O3 film measured at excitation energy densities of 51, 100 and 159 μJ/cm2 (shown as 25, 49, 78 nJ respectively). The signal sizes have been scaled by the corresponding pump powers to reflect the relative injection yield. The inset shows the data at longer time scale. | 125 |
| Figure 7.5 | Transient visible absorption spectra of RhB/In2O3 at delay times (a) -1.5 to 5 ps and (b) 10 ps to 1 ns after 532 nm excitation. The static absorption spectrum of RhB ground state (GSA, black solid curve) has been inverted and scaled for better comparison with the bleach. The legends indicate delay time in units of picoseconds. | 127 |
| Figure 7.6 | Comparison of the growth of the IR absorption of injected electrons (filled circles) and decay of the stimulated emission (SE, open circles) of excited RhB molecules in RhB/In2O3. The SE signal has been displaced vertically and normalized for better comparison. The good agreement confirms the process of electron injection from RhB excited state to In2O3. | 128 |
| Figure 7.7 | Comparison of the recovery of RhB ground state bleach (red open circles) with the decay of cation absorption (black squares) and the IR absorption of injected electrons (blue filled circles). The ground state bleach signal has been inverted for better comparison. | 129 |
| Figure 7.8 | UV-vis spectra of RhB/SnO2 films at three different coverage levels (OD =0.1, 0.2 and 0.43 at 551 nm for samples 1, 2, 3, respectively). All spectra were normalized to the same peak height for better comparison. The inset shows their original spectra. | 130 |
| Figure 7.9 | Transient IR absorption kinetic traces of RhB/SnO2 films 1-3. The inset shows the data at longer time scale. The signal sizes have been normalized to correspond to the same number of absorbed excitation photons. | 131 |
| Figure 7.10 | Kinetic traces of RhB/SnO2 films measured at excitation energy density of 96, 153 and 304 μJ/cm2 (shown as 47, 75 and 149 nJ, respectively). The signal sizes have been scaled by the corresponding pump power. The inset shows the same transient data up to 500 ps. | 132 |
| Figure 7.11 | Transient visible absorption spectra of RhB/SnO2 at indicated delay times (a) -1.5 to 5 ps and (b) 10 ps to 1 ns after 532 nm excitation. The static absorption spectrum of RhB ground state (GSA, black solid curve) has been inverted and scaled for better comparison with the bleach. | 133 |
| Figure 7.12 | (a) Comparison of the formation kinetics of the IR absorption of injected electron in SnO2 (filled circles) with decay kinetics of the stimulated emission of RhB excited state in 600-650 nm region (open circles) in RhB/SnO2. The SE signal has been displaced vertically for better comparison. (b) Comparison of the decay of RhB ground state bleach (inverted, open circles), RhB cation absorption (squares) and the injected electron IR absorption (filled circles) observed at later time delays. | 134 |
| Figure 7.13 | (a) UV-vis spectra of RhB/ZnO films at two different coverage levels: low coverage (0.2 OD) and high coverage (0.58 OD). The spectra were normalized to the same peak height for better comparison. The inset shows the original spectra. (b) Transient IR absorption kinetic traces of RhB/ZnO films at low and high coverage. The inset extends the data to 500 ps. The signal sizes have been scaled to correspond to the same number of absorbed excitation photons. | 136 |
| Figure 7.14 | Transient IR kinetic traces of RhB/ZnO films measured at excitation energy densities of 225, 531 and 2450 μJ/cm2 (shown as 0.11, 0.26 and 1.2 μJ, respectively). The signal sizes have been scaled by the pump power to reflect the relative injection yield. | 137 |
| Figure 7.15 | Transient visible absorption spectra of RhB/ZnO at indicated delay times (in units of ps) after 532 nm excitation, (a) -1.5 to 50 ps, and (b) 50 ps to 1 ns. The static absorption spectrum of RhB ground state (GSA, black solid curve) has been inverted and scaled for better comparison with the bleach. | 139 |
| Figure 7.16 | (a) Comparison of the IR absorption of injected electrons (filled circles) and the decay of stimulated emission of RhB at 600-650 nm (open circles) in RhB/ZnO. The good agreement suggests that excited RhB depletes through electron transfer to ZnO, and other decay pathways are negligible. (b) Comparison of the RhB ground state bleach (open circles) and RhB cation absorption (squares) with the IR absorption (filled circles) of injected electrons at later time delays. The bleach signal has been inverted and scaled for better comparison. | 140 |
| Figure 7.17 | IR absorption kinetic traces of RhB on In2O3, SnO2 and ZnO films averaged over multiple trials. All kinetic traces have been normalized at the maximum amplitudes for better comparison. The inset shows the data up to 1ns. | 141 |
| Figure 7.18 | (a) Comparison of electron injection kinetics from Rh101, Rh6G, and RhB to In2O3, and (b) Comparison of electron injection kinetics from Rh101, Rh6G, and RhB to SnO2. All kinetic traces have been normalized at the maximum amplitudes for better comparison. The inset shows the data up to 1ns. | 143 |

### List of Tables

Chapter 3

| Table 3I | Fitting parameters for the bleach recovery of CdSe-ReC0A samples with different ratios of ReC0A to CdSe. | 44 |
| --- | --- | --- |

Chapter 5

| Table 5I | Fitting parameters for the fluorescence decay kinetics of CdSe and CdSe-PTZ*Fitting parameters for Fl/semiconductor film injection kinetics averaged over multiple trials. | 75 |
| --- | --- | --- |

Chapter 6

| Table 6I | Fitting Parameters for the Exciton Bleach Recovery Kinetics of CdSe. | 100 |
| --- | --- | --- |
| Table 6II | Fitting Parameters for MB+ Ground State Bleach Kinetics in CdSe-MB+. | 106 |
| Table 6III | Fitting Parameters for 1S Exciton Bleach Recovery Kinetics of CdSe- MB+. | 107 |
| Table 6IV | Fitting Parameters for the 1P Exciton Bleach Recovery Kinetics of CdSe-MB+. | 108 |

Chapter 7

| Table 7I | Fitting Parameters of the injection kinetics in RhB/semiconductor films. | 143 |
| --- | --- | --- |
| Table 7II | The amplitude weighted lifetime of the injection kinetics in Rh dyes/semiconductor films | 145 |